## Slide 1
an oral presentation on the theme
Building materials: structure, properties, technologies, equipment
and Additive technologies
Advancing 3D printing of concrete using heat-cured geopolymer
International scientific and practical conference on
Materials science, forming technologies and equipment 2023
(ICMSTE 2023)
Presented by
Prof. Sandeep Chaudhary
Indian Institute of Technology Indore
Indore, India - 453552

## Slide 2
Our team
2
Sanchit Gupta
Department of Civil Engineering,
Indian Institute of Technology Indore, India
Astha Sharma
Department of Civil Engineering,
Indian Institute of Technology Indore, India
Dr. Georgy Lazorenko
Novosibirsk State University,
Novosibirsk, Russia
Platov South-Russian State Polytechnic University (NPI),
Rostov Region, Novocherkassk, Russia
Rostov State Transport University, Rostov-on-Don, Russia
Prof. Sandeep Chaudhary
Department of Civil Engineering,
Indian Institute of Technology Indore,India

## Slide 3
3D printing of concrete reduces material wastage and is considered sustainable solution for construction. [2,4]
In construction, 3D printing is possible only through specialized mixture which has
  1.5-2.0 times cement
  High dosage of VMA and SP
  Nano SCMs and fibers are often used
  Typically designed without coarse aggregate
This drastically increases the cost and associated CO2 emissions.
3D printing saves material, but the specialized mixture is less sustainable.
3D printing and its challenges
3
Video Source: https://www.youtube.com/watch?v=vL2KoMNzGTo&ab_channel=InsiderArt
Video. 1. 3D printing of building materials

## Slide 4
Redefining 3D printing equipment
To improve the sustainability of 3D printing, it suggested to redefine the printing process using heat cured geopolymers.
Geopolymer will remain liquid till the application of heat (active control of rheology).
Geopolymer in liquid state can be used to ensure good extrusion and homogeneity.
Heat curing can be used to ensure thixotropy and buildability.
The redefined process can make the associated material and 3D printing more sustainable.
4
Fig. 1. 3D printing of geopolymer concrete using heat as an active control
Laser for heat application
Solidified geopolymer
Platform to support printed structure
Vat of geopolymer (liquid state)

## Slide 5
Rheological investigation
Design mix 0.25 NaOH sol. (4M/6M) : 0.25 Na2SiO3 sol. : 1.00 Precursor (GGBS/FA)
Rheology measured using dynamic shear rheometer in a parallel plate arrangement, having heating plate at bottom.
Constant shear rate of 1 s-1 was applied for 1 hour (3600 s). Low shear rate to limit breakdown.
3 temperature profiles applied:
  Constant C
  Constant C
  C for 1800 s, C to C in 300 s and C for 1500 s
5
GGBS 4M
GGBS 6M
FA 4M
FA 6M
2 Precursor
2 Activation solution
Chart: Time (s)
4 types of geopolymers
Dynamic shear rheometer
3 different heating profile
Fig. 2.
Testing protocol

## Slide 6
Results
At 20 °C, all geopolymers showed low shear resistance (Fig. 4) (thixotropy 0.014 Pa/s).
At 60 C, all geopolymers showed increased shear resistance, due to geopolymerization. (highest thixotropy ~125 Pa/s for GGBS 4M).
GGBS is a better precursor than FA for the given activation solution.
Activation solution prepared with 4M NaOH shows greater increase in shear resistance.
GGBS 4M has the highest compatibility for heat-curing-based 3D printing.
6
Chart: Time (s)
Chart: Time (s)
Fig. 4. Rheology at C (magnified scale)
Fig. 3. Rheology at C
GGBS
FA

## Slide 7
Results (contd.)
Applying heat curing after an interval (1800 s + 300 s) time shows similar peak value of shear resistance.
Delayed heat application took a slightly longer time for attaining the peak shear resistance value (Fig. 8).
The delay may be a result of time required for the sample to heat up.
7
Chart: Time (s)
Fig. 8. Effect of time
Temperature 60 C from start
Temperature 60 C from t=2100 s

## Slide 8
Demonstration of active control
8
1. Preparation of vat
Geopolymer poured in a flat plate/tray, which acts as a single layer of vat.
2. Heat curing of
selected area
Heating of selected area of geopolymer using a heat gun and circular stencil.
3. Heat cured area solidified
Heat cured area solidified. Visible differences between cured and flowable geopolymer.
Solidified/printed shape after draining of non-printed (flowable) cement paste.
4. Solid/ liquid separation
Solid
Flowable
Geopolymer slurry
Circular
Stencil
Heat gun
Printed circle
Fig. 10. Demonstration of heat curing as active control for 3D printing

## Slide 9
Conclusion
The present study demonstrates the potential of heat curing for advancing 3D printing in the field of building materials.
  Results show that the rheology of a geopolymer is dependent on its composition (precursor type, activation solution) and exposure temperature.
  Demonstrated geopolymer (GGBS 4M) shows very little shear resistance (≤100 Pa) at room temperature (20 °C) and very high shear resistance (>20,000 Pa) under heat curing (60 °C).
  Transition from a liquid-like (low shear resistance) to a solid-like (high shear resistance) state can be achieved by the application of heat at any point in time.
  Heat curing has been demonstrated for active 3D printing of geopolymer.
The rheological investigation and demonstration provide a proof of concept for heat-curing-based 3D printing, which can be used to develop advanced instruments for the 3D printing of building materials.
9

## Slide 10
References
G.H. Ahmed, A review of “3D concrete printing”: Materials and process characterization, economic considerations and environmental sustainability, J. Build. Eng. 66 (2023) 105863. https://doi.org/10.1016/J.JOBE.2023.105863.
Z. Pan, D. Si, J. Tao, J. Xiao, Compressive behavior of 3D printed concrete with different printing paths and concrete ages, Case Stud. Constr. Mater. 18 (2023) e01949. https://doi.org/10.1016/J.CSCM.2023.E01949.
K.A. Ibrahim, G.P.A.G. van Zijl, A.J. Babafemi, Influence of limestone calcined clay cement on properties of 3D printed concrete for sustainable construction, J. Build. Eng. 69 (2023) 106186. https://doi.org/10.1016/J.JOBE.2023.106186.
B. Wang, X. Yao, M. Yang, R. Zhang, J. Huang, X. Wang, Z. Dong, H. Zhao, Mechanical Performance of 3D Printed Concrete in Steam Curing Conditions, Materials (Basel). 15 (2022) 2864. https://doi.org/10.3390/ma15082864.
J. Essmeister, L. Schachtner, E. Szoldatits, S. Schwarz, A. Lichtenegger, B. Baumann, K. Föttinger, T. Konegger, Polymer-derived Ni/SiOC materials structured by vat-based photopolymerization with catalytic activity in CO2 methanation, Open Ceram. 14 (2023) 100350. https://doi.org/10.1016/J.OCERAM.2023.100350.
Y.A. Al-Noaimat, S.H. Ghaffar, M. Chougan, M.J. Al-Kheetan, A review of 3D printing low-carbon concrete with one-part geopolymer: Engineering, environmental and economic feasibility, Case Stud. Constr. Mater. 18 (2023) e01818. https://doi.org/10.1016/J.CSCM.2022.E01818.
10

## Slide 11
Building material lab at IIT Indore
Thank you for your time
11
Brick manufacturing unit
Paver block machine
Dynamic shear rheometer