## Slide 1: Features of the technology for producing multicomponent ferropiezoelectric materials
S.I. Dudkina, L.A. Shilkina, L.A. Reznichenko
Southern Federal University Research Institute of Physics

## Slide 2: Relevance
Most of the known industrially developed ferroelectric piezoelectric materials (FPM) are based on multicomponent systems (MS) of solid solutions. This is due to the possibility of realizing in them a large assortment of compositions with various properties, with increasing efficiency and improving manufacturability. This is what determined the prospect of MS for the search for new functional materials with special electrical (ferroelectric piezoelectric) and/or magnetic properties.
2
Southern Federal University Research Institute of Physics

## Slide 3: Southern Federal University Research Institute of Physics
Our many years of research in the field of physical materials science led to the creation of the FPM series (in ceramic version) based on lead titanate and the well-known binary system PZT (Pb(Ti, Zr)O3, as well as environmentally friendly FPM based on niobates of alkali metals, "overlapping" almost all known piezoelectric applications. FPMs have also been developed with the participation of lead titanate modified with rare earth elements (REE) for flaw detection of the equipment, medical diagnostic devices, etc. All FPMs were obtained by one- or two-stage solid-phase synthesis followed by sintering either by conventional ceramic technology or by hot pressing.
3

## Slide 4: Southern Federal University Research Institute of Physics
When working with MS or compositions with introduced dopants, special attention is paid to the state of the ceramic frame - its homogeneity, defectiveness, strength, since the electrical properties of objects depend on this. However, the technical capabilities of X-ray equipment used in research laboratories to control the impurity composition and crystal structure of objects do not allow to estimate with sufficient accuracy the presence of small (<3 %) amounts of unreacted components and to establish the completeness of the reaction, which is especially important in the case of MS.
4

## Slide 5: Southern Federal University Research Institute of Physics
Purpose of work:
Development of a technological method that allows to obtain a single-phase synthesized base corresponding to a given stoichiometric composition for the manufacture of high-density ceramics.
5

## Slide 6: Southern Federal University Research Institute of Physics
Objects and methods of obtaining them
The objects of study in this work are solid solutions based on PbTiO3 modified with rare-earth oxides. The studied solid solutions were prepared by solid-phase synthesis and subsequent sintering by hot pressing.
6

## Slide 7: Southern Federal University Research Institute of Physics
Object research methods
X-ray studies were carried out by powder diffraction using a DRON-3 diffractometer (Сока – radiation).
Electrophysical parameters - relative permittivity of polarized samples, ε33Т/ε0 , electromechanical coupling coefficients of radial, Kр, and thickness, Kt, vibration modes, mechanical quality factor, Qм; – determined according to IEEE Standard on Piezoelectricity ANSI/IEEE Std 176-1987 based on measurements of the material characteristics using an Agilent 4980A precision LCR meter and a Wayne Kerr 6500B precision impedance analyzer.
7

## Slide 8: Southern Federal University Research Institute of Physics
Experimental results and discussion
A technological method has been developed for the production of FPM based on lead titanate with additives of rare-earth oxides, which is presented step by step by the example of the composition Pb0.88Nd0.1Ti0.92Mn0.02In0.06O3. The product synthesized at 1123 K for 2 hours is divided into a series of samples and subjected to successive firing for 2 hours, starting from the synthesis temperature with a fixed step (25–50 degrees). After each firing, X-ray control of the absence of ballast phases is carried out, the symmetry of the crystal lattice is determined and the parameters of the unit cell are calculated. According to the results of the study, the optimal firing temperature T0 is selected, above which the change in structural parameters stops, that is, complete dissolution of the original components occurs.
8

## Slide 9: Southern Federal University Research Institute of Physics
After that, additional firing of the entire mass of the synthesized product is carried out for 1.5–2.0 hours at a temperature lying in the range (Т0 ± 25) deg. (For the indicated composition Т0 = 1503 K). Next, the samples are sintered in an air atmosphere by the method of hot pressing.
The use of the developed technological procedure for the production of ceramics based on lead titanate with additives of rare-earth oxides leads to an increase in the coefficient of electromechanical coupling (Kt) and anisotropy of piezoelectric parameters (Kt/Kр) with practically invariable values of the dielectric constant (ε33Т/ε0) and mechanical quality factor (Qм) of objects. The table shows comparative data for materials made by two methods.
9

## Slide 10: Southern Federal University Research Institute of Physics
10
Parameters | Material manufacturing method | 
 | developed | traditional
Kt | 0.24-0.46 | 0.18-0.40
Kt/Kр | 4.5-8.0 | 3.0-3.6
ε33Т/ε0 | 208-250 | 205-245
Qм | 400-1800 | 410-1750
An improvement in the electrical properties of materials based on the Pb(Ti,Zr)O3 system and alkali metal niobates prepared by the developed method was also observed.

## Slide 11: Southern Federal University Research Institute of Physics
Conclusions
A method is proposed for additional heat treatment of the synthesized product at a temperature corresponding to the termination of the change in the parameters of the unit cell of the samples. The developed technological method for the manufacture of laboratory samples is considered step by step by the example of the composition Pb0.88Nd0.1Ti0.92Mn0.02In0.06O3.
It is shown that the proposed method can also be used in the manufacture of other ceramics based on lead titanate with the participation of REE oxides (La2O3, CeO2, Pr2O3, Sm2O3, Gd2O3, Tb2O3, Yb2O3), as well as compositions with the participation of PZT.
11

## Slide 12: Southern Federal University Research Institute of Physics
The materials obtained using the proposed method have improved characteristics in comparison with similar ones realized in materials manufactured by the traditional method: high values of Kt and anisotropy of piezoelectric parameters (Kt/Kр) with practically invariable values of dielectric constant (ε33Т/ε0) and mechanical quality factor (Qм) of objects.
The developed materials and methods for their manufacture are promising for the creation of electronic devices, including high-frequency electroacoustic transducers, devices for flaw detection of equipment, medical diagnostics devices, etc.
12

## Slide 13: Southern Federal University Research Institute of Physics
Thank you for attention!
13